目录

GY-DBD-PP 100 打包带机用途和特点Usage and characteristics	2

GY-DBD-PP-100 打包带机主要技术参数Main Technical Parameters	2

1、挤出机 Extruder	2

2、第一牵引：The first drawing	3

3、热烘箱：Heating oven	3

4、第二牵引：The second drawing	3

5、压花：Embossing	4

6、卷取：Winding	4

减速箱轴承和油封Reducer bearing and oil seal	4

挤出机操作说明Instructions for extruder operation	5

挤出机故障分析Fault analysis of extruder	7

第一牵引 The first traction	11

热烘箱 Heating oven	13

使用注意事项：Use notice	13

第二牵引The second traction	14

2N精密卷取机	16

产品介绍Product introduction	16

使用注意事项：Use precautions	16

当产品宽度变化时，请更换变距齿轮（见后图）	18

WPK AK6 汇邦温控表调节方法	20

设定温度（SV）调节：Setting temperature (SV) regulation	20

报警温度（P18）设定：Alarm temperature (P18) setting	21

温度修正参数（P13）调节：Temperature correction parameter(P13)regulation	21

自整定（AT）操作：Self-tuning(AT)operation	21

附图  Figures	22

GY-DBD-PP 100 打包带机用途和特点Usage and characteristics

GY-DBD-PP-100打包带机组是生产聚丙烯机用打包带和手用打包带的专用设备。全套机组由挤出、机头、冷却、牵引、加热、拉伸、压花、卷取、电气等10个部分组成 。挤出机螺杆设计特殊，机头模口间隙采用可调式设计，有得于变换产品规格。由于 结构设计合理，因而具有产量高，塑化好，加工适应性强，操作简便，检修容易等优点。

GY-DBD-PP-100 plastic strap making machine is a special equipment for producing polypropylene machine packing belt and hand packing belt. The complete set consists of 10 parts, such as extrusion, head, cooling, traction, heating, stretching, embossing, winding and electrical. The design of extruder screw is special, and the clearance of the die head adopts adjustable design. Due to the reasonable structure design, it has the advantages of high output, good plasticizing, strong processing adaptability, simple operation and easy maintenance.

GY-DBD-PP-100 打包带机主要技术参数Main Technical Parameters

1、挤出机 Extruder

中心高：1000m 螺杆直径：Φ100mm

长径比：30:1   螺杆转速：0-54 r/min

生产能力：130-150 kg/h  电机功率：22KW（变频调速）

电机转速：1470 r/min  加热段数：机筒5区；模具3区

加热功率：30KW  制冷方式与段数：强制风冷，共4段

主机装机容量：57KW  整机重量：2.5T

High: 1000mm.  Screw diameter: Φ100mm.

Length to diameter ratio: 30:1.   Screw speed: 0-54r/min.

Production capacity: 130-150kg/h.  Motor power: 22KW(frequency control).

Motor speed: 1470r/min.    Heating section: cylinder 5 zone, mould 3 zone.

Heating power: 30KW.

Refrigeration mode and number of section: forced air cooling, 4 segments in total.

Main machine installed capacity:57KW

Weight:2.5T

2、第一牵引：The first drawing

电机功率；1.1KW，变频调速，牵引速度1.25-12.5m/min

Motor power 1.1KW, frequency control, traction speed 1.25-12.5m/min.

3、热烘箱：Heating oven

加热功率：4KW*4=16KW 380V, 打水电机功率：1.1KW

Heating power: 4KW*4=16KW 380V, water dry motor power: 1.1KW

4、第二牵引：The second drawing

电机功率：5.5KW，变频调速，牵引速度12.5-110m/min

Motor power 5.5KW, frequency control, traction speed 12.5-110m/min

5、压花：Embossing

电机功率：1.1KW，变频调速，速度12.5-110m/min

Motor power 1.1KW, frequency control, speed 12.5-110m/min

6、卷取：Winding

电机功率：2N力矩电机，速度约110m/min

Motor power 2N torque motor, speed about 110 m/min.

减速箱轴承和油封Reducer bearing and oil seal

| 轴承 bearing |  |  | 油封 oil seal |  |  |
| --- | --- | --- | --- | --- | --- |
| 轴承型号 bearing model | 轴承尺寸 bearing size | 数量 quantity | 位置position | 油封尺寸 oil seal size | 个数quantity |
| 29424+22224 | Φ120×Φ250×78 | 1 | 输出轴法兰处 output shaft flange | Φ130×Φ160×12 | 2 |
|  | Φ120×Φ215×58 | 1 |  | Φ258×7（0型圈） | 2 |
| 22222 | Φ110×Φ200×53 | 1 | 输出轴后压盖处 output shaft’s rear gland | Φ90×Φ120×12 | 1 |
| 32312 | Φ60×Φ130×48.5 | 2 |  |  |  |
| 32310 | Φ50×Φ110×42.25 | 2 | 输出轴压盖处 output shaft gland | Φ50×Φ70×8 | 1 |

挤出机操作说明Instructions for extruder operation

1、挤出机电源电压：AC三相380V+N（零线），并注意接上地线。

Extruder power supply voltage: AC three-phase 380V+N (zero line), and pay attention to the ground wire.

2、新机出厂前虽已调效过温度，但在实际生产时，按所须温度用温度计再核对一次，以保证生产顺利进行。

Although the new machine has already adjusted the temperature before it leaves the factory, in the actual production, it shall be checked again with a thermometer according to the required temperature to ensure smooth production.

3、开机前加热至预定温度后，保温三十至四十分钟，保证模头和螺杆的温度足够物料塑化。

After heating to the predetermined temperature before starting the machine, keep the heat for 30 to 40 minutes to ensure that the temperature of the die head and screw is enough to plasticize the material.

4、开机前检查减速箱润滑油高度，不够时添加齿轮油15#机油。减速箱和机筒水套要加水冷却。

Check the lubricating oil height of the reducer before starting up, and add 15# gear oil when insufficient. The reducer box and cylinder water sleeve should be cooled by water.

5、出厂前，风机和主机方向都检查好了，但到新厂接线后，要重新检查风机和主机方向，方向相反要调换电源线。

Before leaving the factory, the direction of the fan and the host machine have been checked, but after connecting in the new factory, the direction of the fan and the host should be re-checked, if in the opposite direction should be change the power line.

6、新机使用两个月后，一定要更换机油，以后半年至八个月更换一次。

After using the new machine for two months, the oil must be replaced, and the oil should be replaced once in the next six months to eight months.

7、在生产过程中，防止工具或杂物掉入料斗，以免损坏螺杆。

In the process of production, tools or sundries should be prevented from falling into the hopper to avoid damaging the screw.

8、开机时启动电机，低速空转约半分钟，无异常时投放少量原料，待出料口有出料后，再正常生产。

Start up the motor , and idle at low speed for half a minute. When the machine is not abnormal, put in a small amount of raw material, after product discharge, it will be able to produce normally.

9、正常生产时主机电流不大于额定电流，没有异常响声。

During normal production, the host current is not greater than the rated current, and there is no abnormal noise.

10、生产时要注意各区温度，主机电源、出料情况是否正常。

Pay attention to the temperature in each zone during production, and whether the power supply and discharge are normal.

11、出料有焦黄时，要停机清理螺杆和模具，注意温度。

When the discharge is brown, stop the machine to clean the screw and mold, pay attention to the temperature.

12、停机前，排空螺杆内塑料，清理模头，料斗加盖，关电源。

Empty the plastic from the screw, clean the die head, cover the hopper and turn off the power before stop.

挤出机故障分析Fault analysis of extruder

| 故障现象 | 产生原因 | 处理方法 |
| --- | --- | --- |
| 1、启动主电动机时，主电机不动或瞬间停机 | 1、主电动机电源没有接通。 2、加热升温时间不足或加热器不工作造成扭矩过大，使电机过载。 | 1、检查主电路电源接线。 2、检查各段温度显示并查找有关记录，确认预热升温时间。 |
| 2、主电动机转动，但螺杆不转动 | 1、传动带松，打滑。 2、安全键剪切断。 | 1、调整两带轮的中心距。 2、检查安全键，分析切断原因，更换。 |
| 3、螺杆有转速显示但挤不出物料 | 1、料斗没有物料。 2、加料口被异物堵住或产生“架桥”，不能下料。 3、螺杆内掉进金属等坚硬物，堵塞螺槽，不能输送物料。 4、螺杆从加料段根部扭断。 5、螺杆料筒温度过高，螺杆内冷却不良，形成抱轴现象。 | 1、向料斗里加料。 2、排除料斗口的异物或消除“架桥”现象。 3、如确认有硬物进入挤出机内，应停机拆螺杆，排除堵塞硬物。 4、检查从动带轮是否转动，如转动正常且排除了不加料或硬物堵塞，则可能是螺杆扭断，应立即停机拆卸螺杆更换修理。 5、检查螺杆冷动水系统，加大螺杆冷却水量。 |
| 4、挤出制品中有污物 | 1、物料内有污物。 2、挤出机螺杆积碳过多。 | 1、更换物料。 2、清理螺杆，轻者可用螺杆清洗剂直接挤出清理，重者可将螺杆拆卸下来，人工清理。 |
| 5、挤出机主电机电流波动大 | 1、某段加热器不工作，扭矩不稳。 2、主电动机轴承润滑不好或损坏，震动大。 | 1、检查各段加热器是否有损坏，如有，更换，检查各段加热器的接线是否正确或牢固。 2、检查电动机轴承，加润滑剂或更换轴承。 |
| 6、挤出物不稳定 | 1、原料加料口有“架桥”。 2、主电动机转速不均，有波动。 3、加热冷却系统匹配不好或者热电偶误差太大。 | 1、清除料斗口的架桥，检查水套是否加水冷却。 2、检查主电机及控制系统。 3、对加热功率进行调整或检查热电偶的接触情况以及热电偶是否损坏，必要时更换热电偶。 |

Fault analysis of extruder

| Problem | Reason | Solution |
| --- | --- | --- |
| 1. When the main motor is started, the main motor will not work or stop at once. | 1. The power of the main motor is not connected. 2. The insufficient heating time or the heater does not work, resulting in excessive torque and overload of the motor. | 1. Check the power connection of the main circuit. 2. Check the temperature display of each section and find relevant records to confirm the preheating and heating time. |
| 2.The main motor turns, but the screw doesn’t . | 1. The transmission belt is loose and skidding. 2. The safety key is cut off. | 1. Adjust the center distance of the two belt wheels. 2. Check the safety key, analyze the reasons for cut-off and replace it. |
| 3. The screw has a rotational speed display but cannot squeeze out the material | 1. There is not materials in the hopper. 2. The feeding port is blocked by foreign matter or produces a "bridge", and cannot feed. 3. Drop metal and other hard objects into the screw rod, block the screw slot, and cannot transport materials. 4. Screw is twisted off from the root of feeding section. 5. The temperature of the screw barrel is too high, and the internal cooling of the screw is not good enough to form the axle holding phenomenon. | 1. Feed the hopper. 2. Eliminate foreign matter at the hopper or bridge phenomenon. 3. If any hard object is confirmed to enter the extruder, the screw should be disassembled and remove the plugging hard object. 4. Check whether the driven pulley is rotating, if the rotation is normal and no need feeding and no hard material clogging, the screw may be broken, stop the machine and replace or repair it immediately. 5. Check the screw cooling water system and increase the screw cooling water. |
| 4. There is dirt in the extrusion products. | 1. There is dirt in the material. 2. The extruder screw has too much carbon. | 1. Replace material. 2. Clean the screw. the screw with light carbon accumulation can be directly extruded to clean the screw with screw cleaner. The screw with heavy carbon deposition can be removed and manually cleaned. |
| 5. The main motor’s current of the extruder fluctuates greatly. | 1. The heater in a certain section does not work and the torque is unstable. 2. The bearing of the main motor is not well lubricated or damaged, and has a large vibration. | 1. Check whether the heater in each section is damaged, if any, replace it, and check whether the heater wiring in each section is correct or firm. 2.Check motor bearings, add lubricant or replace bearings. |
| 6. Extrusion unstable. | 1.There is a “bridge” at the feed inlet. 2.The main motor speed is not uniform, there is fluctuation. 3. The heating and cooling system does not match well or the thermocouple error is too large. | 1. Clear the “bridge” at the hopper port and check whether the water jacket is cooled by water. 2. Check the main motor and control system. 3、Adjust the heating power or check the or check the contact of thermocouple and whether the thermocouple is damaged. If necessary, replace the thermocouple. |

第一牵引 The first traction

本机用于打包带生产线出料牵引，由电气和机械两部分组成 。电气部分主要是牵引控制和加热控制；机械部分为牵引的机械结构，由电机和传动装置组成 。电机由变频器控制调速，传动装置采用链条传动方式。具有结构精简，操作方便，经济实用的特点。

This machine is used for packing traction in production line, consisting of two parts, electrical and mechanical. The electrical part is mainly traction control and heating control; the mechanical part is the mechanical structure of traction, composed of motor and transmission device. The motor is controlled by a frequency converter, and the transmission device adopts a chain drive mode. It has the characteristics of simple structure, convenient operation, and economic utility.

电机功率：1.1KW，变频调速，牵引速度1.25-12.5m/min

Motor power: 1.1kw, frequency control, traction speed 1.25-12.5m/min

使用注意事项：Use notice

1）本机到厂后由专业电工接好线，调试好再投入生产。

After the machine arrived the factory, it should be connected by professional electrician and debug it , then put into production.

2）严格按规定电源三相380V+N线，接好地线。

Strictly according to the specified power supply three-phase 380V+N line, connect the ground wire.

3）使用应检查、清除机内可能遗留的杂物，检查各螺丝是否松动，如果有需要可加地脚螺丝。

Check and remove the possible debris in the machine before use, check whether all screws are loose, and add ground screw if necessary

4）传动装置要定期加注润滑油。

The transmission device should be regularly filled with lubricating oil.

产品经过牵引轮的环绕方法请参照附图。

Please refer to the attached drawings for the winding method of the product through the traction wheel.

热烘箱 Heating oven

本装置用于打包带生产线拉伸前的加热，由加热、冷却和打水电机组成 。加热装置分为一、二区，共有4条U型加热棒，上下各2条。通过加热棒发热使箱内温度升高，达到拉伸的工艺要求。冷却水槽用于拉伸后产品定型。打水电机用于产品冷却后除去产品上的水。

The device is used to heating before stretching, which consists of heating, cooling and dry water motors. The heating device is divided into one and two zones. There are 4 u-shaped heating rods, 2 above and 2 below. By heating the heating rod, the temperature in the box is increased to meet the technical requirements of stretching. The cooling tank is used to shape the product after stretching. The dry water motor is used to remove water from the product after cooling.

加热功率：4KW×4=16KW 380V，打水电机功率：1.1KW

Heating power: 4KW * 4=16KW 380V, dry water motor power: 1.1kw

使用注意事项：Use notice

1）本装置为加热装置，操作时要注意，以防烫伤

This device is a heating device. Please pay attention to the operation to avoid scalding.

2）加热棒电源两相380V.

The power supply of the heating rod is 380V in two phases

3）使用应检查、清除箱内的杂物。

Check and remove the sundries in the box before use.

产品经过热烘箱的环绕方法请参照附图。

Please refer to the attached drawing for the wrapping method of the product through the hot oven.

第二牵引The second traction

本机用于打包带生产线产品拉伸。由电气、压花和机械三部分组成 ，电气部分主要是拉伸电机控制和压花电机控制；机械部分为拉伸和压花装置的机械结构。拉伸装置由电机和传动装置组成 。电机由变频器控制调速，传动装置采用链条传动方式。压花装置由电机带动，手动调节压花的深度。具有结构精简，操作方便，经济实用的特点。

This machine is used to stretch the product. It consists of three parts: electrical, embossing and mechanical parts. The electrical part is mainly the drawing motor control and the embossing motor control, and the mechanical part is the mechanical structure of the drawing and embossing devices. The drawing device consists of a motor and a transmission device. The motor is frequency control, and the transmission device adopts a chain drive mode. The embossing device is driven by a motor and manually adjust the depth of embossing. It has the characteristics of simple structure, convenient operation, and economic utility.

拉伸电机功率：5.5KW，变频调速，牵引速度12.5-110m/min

压花电机功率：1.1KW，变频调速，牵引速度12.5-110m/min

Drawing motor power: 5.5kw, frequency conversion speed regulation, traction speed: 12.5-110m/min

Embossing motor power: 1.1kw, frequency conversion speed regulation, traction speed: 12.5-110m/min

使用注意事项：Use notice

1）本机到厂后由专业电工接好线，调试好再投入生产。

After the machine arrived the factory, it should be connected by professional electrician and debug it , then put into production.

2）严格按规定电源三相380V+N线，接好地线。

Strictly according to the specified power supply three-phase 380V+N line, connect the ground wire.

3）使用应检查、清除机内可能遗留的杂物，检查各螺丝是否松动，如果有需要可加地脚螺丝

Check and remove the possible debris in the machine before use, check whether all screws are loose, and add ground screw if necessary

4）传动装置要定期加注润滑油。

The transmission device should be regularly filled with lubricating oil.

5）压花装置操作时须小心注意，两边手轮要同时升降，避免两个轮碰撞。

Pay attention to the operation of the embossing device. Both hand wheels should be lifted and lowered simultaneously to avoid collision between two wheels.

产品经过拉伸轮的环绕方法请参照附图。

Please refer to the attached drawings for the winding method of the product through the traction wheel.

# 2N精密卷取机

2N precision coiling machine

产品介绍Product introduction

本厂生产的精密卷取机，用于打包带及丝状产品的收卷。

多年来，该机从开发研制成功到五次改型换代，其结构功能和操作维修都有显著改进，更臻完善；摆线精度和使用寿命显著提高 ，加上本厂有中皆碑的良好售后服务，深受广大新老客户欢迎。

The precision coiling machine produced by our factory is used for winding the packing belt and filamentary products.

Over the years, the structure function and operation and maintenance of the machine have been improved remarkably from the development to the five times upgrading. The cycloid precision and service life have been greatly improved, and the good after-sales service of our factory has been welcomed by new and old customers.

使用注意事项：Use precautions

1）本机到厂后由专业电工接好线，调试好再投入生产。

After the machine arrived the factory, it should be connected by professional electrician and debug it , then put into production.

2）严格按规定电源三相380V+N线，接好地线。

Strictly according to the specified power supply three-phase 380V+N line, connect the ground wire and run according to the directions.

3）使用应检查、清除机内可能遗留的杂物，检查各螺丝是否松动，如果有需要可加地脚螺丝

Check and remove the possible debris in the machine before use, check whether all screws are loose, and add ground screw if necessary

4）客户如有需要，请先作联系，我厂即可根据用户具体要求 进行改装。

If need, please contact us first, our factory can refit according to the user’s specific requirements.

5）每天要加油一次（用二硫化钼类润滑脂，齿轮和链轮、左右螺杆、油嘴位置在轴承座有“油”标志处）。

oiling once a day (with molybdenum disulfide grease, gear and chain wheel, left and right screw and oil nozzle are marked with "oil" at the bearing pedestal).

6）严禁工具、硬物、粘性物料混入机内运转。

It is strictly prohibited to mix tools, hard objects and sticky materials into the machine for operation.

7）工作过程中，机器若有异常，应立即停机检查，排除故障。

During the working process, if the machine is abnormal, it should stop immediately for checking and troubleshooting.

8）开机时手不要放入旋转盘里面。

Do not put the hand into the rotating disk when you start the machine.

9）使用一段时间后，要调节皮带和链条的松紧度。

Adjust the tightness of the belt and chain after a period of use time

10）本机外观若有改动，恕不另行通知。

The appearance of this machine is subject to change without notice.

当产品宽度变化时，请更换变距齿轮（见后图）

When the product width changes, please replace the variable pitch gear(see the following figure)

1、松开固定螺丝，移动摆臂；

Loosen the fixing screw and move the swing arm;

2、松开变距齿轮；

Loosening the variable pitch gear;

3、更换合适的变距齿轮；（见表格）

Replace the appropriate variable pitch gear; (see table)

4、移动摆臂至原位，紧定固定螺丝；

Move the arm to the original position and tighten fixing screw;

5、加黄油于齿轮上。

Add butter to the gear.

# WPK AK6 汇邦温控表调节方法

WPK AK6 Huibang temperature control meter adjustment method

设定温度（SV）调节：Setting temperature (SV) regulation

按SET键1秒，下排数字闪烁，按∨或∧键，改变闪烁的数字，完成后再按SET键1秒。

Press the SET key 1 second, the next row of numbers twinkle, press ∨or∧ key to change the number of twinkle, and then press the SET key for 1 second after finish.

报警温度（P18）设定：Alarm temperature (P18) setting

按住SET键2秒，重复按∧键，显示P18，按一下SET键，按∧或∨键，修改SV值为2，按SET键即可。

Press the SET key for 2 seconds, repeat press ∧key, display P18, press the SET key, press∧key or ∨key , modify the SV value to 2, then press the SET key.

温度修正参数（P13）调节：Temperature correction parameter(P13)regulation

按住SET键2秒，重复按∧键，显示P13，按一下SET键，按∧或∨键，修改SV值，按SET键即可。当显示温度与水银温度计出现误差时，可以用这个参数修正。方法是在参数值的基础上加上或减去显示温度和测量温度的差值，改好后按SET键5秒。

Press SET key for 2 seconds, repeat press∧key, show P13, press the SET key, press ∧ or ∨, modify the SV value, press the SET key. This parameter can be used to correct errors in the display temperature and mercury thermometers. The method is to add or subtract the difference between the display temperature and the measured temperature on the basis of the parameter value, and then press SET key for 5 seconds after modification.

自整定（AT）操作：Self-tuning(AT)operation

长按∨键约5秒，进入自整定，PV值会一直闪烁，直到自整定结束。自整定后控制效果更好。

Press the∨key about 5 seconds and enter the self-tuning. The PV value will always flicker until the self tuning is finished. The control effect is better after self tuning.

附图  Figures